## Slide 1
Bragg Diffraction Based Imaging Techniques
Dec 5th 2017, Annecy
Tobias Schülli,
ESRF Head of the X-ray Nanoprobe group
Scientist in charge of Beamline ID01
The European Synchrotron ESRF
Notes: Who is a spectroscopist, diffraction ? Material scientist ? Good at QM ?

## Slide 2
ESRF/ ID01 team

## Slide 3
Science with x-rays at the heart of the French Alps, at the eSRF in Grenoble, France
ESRF Upgrade phase I: 2009-2015: construction of new beamlines
ESRF Upgrade phase II (EBS): Extremely Brilliant Source upgrade (40-100 times more brilliance)
operational in 2020
The European Synchrotron ESRF
Things you should know after this lecture:
-What a Lorentz contraction is
-Why lenses cannot simply be replaced by computers
-Why there are no good x-ray optics
-What Joan Baez’ ties to x-ray science are
-That continents are drifting
-The age of the universe
-How to make the difference between a star and a planet

## Slide 4: ouTline
-The brilliance of synchroton light sources
-Nano focused x-rays: rapidly evolving tools for (nano) science
-State of the art nano (diffraction) imaging at the ESRF
-Outlook: tomorrows’ light-sources

## Slide 5: Light emission by accelerated charges
Larmors formula (19th century): irradiated power by accelerated charges:
Relativistic version (total power):
describes e.g. the Lorentz contraction or the time dilation (twin paradoxon etc…)
Is the ratio between total energy and “rest energy”
60 kV (Lab source electron gun): 1.05…1.2
ESRF (6 GeV): 11750 ~ 104

## Slide 6: Light emission by accelerated charges
Classical result (Linear acceleration ):
Propagation
Acceleration
Directional emission characteristics by an accelerated charge (dipole)
Notes: 10 mins at the end

## Slide 7: Light emission by accelerated charges
Relativitic (X-ray tube, Cathodic tube):
Propagation
Acceleration
Directional emission characteristics by an accelerated charge (dipole)
Notes: 10 mins at the end

## Slide 8: Light emission by accelerated charges
Highly relativistic case
Propagation
Acceleration
Directional emission characteristics by an accelerated charge (dipole)
Opening angle
Notes: 10 mins at the end

## Slide 9: Light emission by accelerated charges
Highly relativistic case & circular motion
Propagation
Acceleration
Directional emission characteristics by an accelerated charge (dipole)
Opening angle
Notes: 10 mins at the end

## Slide 10: Light emission in a Synchrotron: circular motion
Highly relativistic case & circular motion
“Flash” every time an electron is passing by:
“ Bending magnet radiation
Notes: 10 mins at the end

## Slide 11: Wigglers: magnetic multipoles: “many bending magnets”
Wigglers: sum of N bending magnets: gain = N
Notes: 10 mins at the end

## Slide 12: Undulators: ”Resonators”
Undulators: stimulated emission, N magnetic pairs
Adapt Magnetic field (or periodicity) that angular variation of the electron beam smaller than
Gain = N2 11 orders of magnitude more brilliance than from anodes
Supplies a self collimated line spectrum
Wavelength ?
1 cm (10-2 m), Lorentz contraction g = 104
For the electrons it becomes 1 mm (10-6 m) -> Infrared
Sample is standing still with respect to electrons
-> Lorentz contraction (“blue shift”) 10-6 m ->10-10 m = X-rays
Notes: 10 mins at the end

## Slide 13: Synchrotrons supply new experimental tools
Where are new metrology tools needed ?
“Easy” to study systems
Challenging systems:
Crystals, systems in their ground state, static systems
Systems far from equilibrium (dynamic systems, metastable and transient states)
Time resolution
Spatial resolution
Complex systems as fully processed microelectronic devices, functional nano-materials, life
Notes: 10 mins at the end

## Slide 14: The dilemma of x-ray optics
Polarized electron clouds=driven harmonic oscillators
Amplitude
For w<<w0: P=const. (does hardly vary with w)
eyeglasses work for all colours,
In this regime, refraction is almost achromatic
For w>>w0: P~1/w2, thus P-> 0
Refraction in the x-ray regime is very weak and highly chromatic!!,
n 0.99999..
The refractive index is expressed as n
c=polarizability
Polarization P=c*E

## Slide 15: Development of x-ray optics
Mirrors:
P. Kirkpatrick (1894-1992)
Baez (1912-2007)
Can only be used for focusing
Refractive lenses:
Excellent imaging devices
Diffractive optics: Fresnel zone plates
Excellent focusing devices
Resolution limit of typical x-ray optics hardly better than 50 nm,
Much worse than the potential offered by the x-ray wavelength of <0.1 nm
All x-ray optics have poor numerical apertures !

## Slide 16: X-rays and spatial resolution
Straightforward approach: focused X-ray beams (~ 20 nm to few 100 nm today)
Powerful scanning probe techniques.
Focussed X-ray beam
Absorbtion contrast, phase contrast (imaging)
Spectroscopic information (fluorescence, photoemission,..)
Diffraction and scattering (atomic structure)
EXAFS spectrum

## Slide 17: Diffraction (and) imaging techniques
Imaging: spatial resolution ~sub mm (traditional sources)
X-ray imaging:
1st application of x-rays, applied in hospitals less than one year after their discovery 1896. 1st nobel price in physics (Röntgen)
Diffraction
Proof of the wave nature of x-rays and the atomic structure of matter: Nobel prices 1914 (Laue) &1915 (Bragg)
….seeing is believing…
Diffraction : spatial resolution traded in for angular resolutions

## Slide 18: Scanning Probe techniques
Object: a flat two dimensional powder…
Slide courtesy: W. De Nolf, M. Cotte (ESRF, ID21)

## Slide 19: Bragg Diffraction imaging (ID01 beamline ESRF built 2013-2015)
Full field techniques
Coherent reconstruction techniques
Scanning techniques
100 nm
60 nm
5 nm

## Slide 20: Nanodiffraction (K-MAPPING)
3D reciprocal space information from 2D surface
Big data (few 100 images/s, TB in hours)
Area Detector
rotate
Area Detector
δ2θ
δtilt

## Slide 21: Mapping of orientation and strain in functional layers
Relative strain levels of Da/a 10-6 can trace a landscape
= we can “see” a DT of a few K potentially in buried systems (working devices)
Spatial resolution: 50-100 nm (today)
G. A. Chahine, et al., J. Appl. Cryst. (2014)
Δd/d < 10-5
Tilt < 10-3 °
3D Reciprocal Map in each pixel

## Slide 22: Diffraction imaging: cross hatches in graded buffers
After growth
After polishing
Light interference microscopy
Scanning x-ray diffraction microscopy: Tilt maps
Surface roughness
Lattice undulations
Zöllner, et al.:
Appl. Mat.&Interf. 2015

## Slide 23: Diffraction imaging: full field
Full field technique
Resolution ultimately limited by numerical aperture of the
Imaging optics
Sub 100 nm within reach
Diffracted signal
Detector

## Slide 24
FULL FIELD DIFFRACTION MICROSCOPY (USERS SINCE APRIL 2017)
Source: Felix Marschall (2014)
FFXDM:
in situ
sample-detector distance: 6.5 m
Incoming X-rays
T. Zhou et al.

## Slide 25: Operando cycling of a Si-Li battery
FFXDM:
in situ
sample-detector distance: 6.5 m
Si
Li
V
T. Zhou et al.
Time resolution today: sub second
Spatial resolution: 100nm (30 nm tested)
Stress evolution on the electrode during lithiation:
100 mm
Image contrast produced
by lattice strain on the
Si electrode

## Slide 26: Full field strain imaging
Strain in Si device (caused by Cu/Si interfaces) :
Strain pattern in a “homogenous” thin film
More examples in the Talks of T. Zhou and P. Reiss

## Slide 27: From full field to coherent diffraction imaging (CDI)
Full field technique
Resolution ultimately limited by numerical aperture of the imaging optics:
Sub 100 nm within reach
Detector
What we have
What we want
Dx=

## Slide 28: Coherent Diffraction imaging (CDI)
Coherent Diffraction Imaging:
Detector
What we can do
Theory of optics is very well known.
-> Measure all emitted rays from the sample and replace the lens by a computer to calculate the image
The physics of resolution remains the same
Abbé limit Dx=
2a
Instead of the lens we need a detector with a large opening angle.

## Slide 29: Coherent Diffraction imaging (CDI)
Detector
Another Problem : Waves have amplitudes and phases: they interfere to form an image;
Refraction (as in a real lens) preserves the phase information, crucial for the image
Detection measures only the intensity (number of photons) and not their phase
From a quantum mechanical point of view, refraction (preserves Dp) by a lens cannot be replaced by detection (destroys Dp): Equivalence between Abbé and Heisenberg.
The loss of phase information cannot be recovered by a computer.
We have thus to know the phase beforehand.
The sample has to be illuminated with photons that are all in phase with each other
This is the definition of a coherent beam

## Slide 30: Coherence length of a source
Source size S
S
Distance D of observer

## Slide 31: Coherence length of a source
Source size S
S
Transverse Coherence length L
Distance D of observer
Wavelength l
Coherence length: L~l*D/(2*S)

## Slide 32: Coherence length of a source
Transverse coherence length of a source: L~Dl/S, with S= source size, D=distance from the source,
Distance Planet Mars: 4exp12 m
l light: 5exp-7m
Diameter mars:6exp6 m
->coherence length L(Mars)=0.16 m
Distance typical star: 100 light years = 5e17 m
l light: 5e-7 m
Diameter star (sun):1e9 m
-> coherence length L(star)=125 m

## Slide 33: Coherent flux of a source
Flux available for “normal” light imaging and coherent diffraction x-ray imaging:
5 Watt LED: 1019 photons/second (incoherent but with optics we can use them all)
ESRF coherent flux: 1011 photons/second (@ 8keV ) -> 1019 photons in 1 year
X-ray tube coh. flux: few photons/second,1019 photons in 1010 years (the age of this world)
Coherent fraction @ ESRF today @ 8 keV: 0.3 %

## Slide 34: Coherent beams, preparation
Source
Light beam
Aperture corresponding to coherence length
Coherent beam
Coherence length: L~l*D/(2*S)
Example for X-rays (ESRF): Source size: 20 mm x130 mm, wavelength 0.1 nm, means:
At 100 m from the source L= 0.4 mm 0.07 mm
optics
Coherent spot
100 m
0.1-0.3 m
Coherent fraction @ ESRF today @ 8 keV: 0.3 %
The ideal coherent diffraction imaging beamline must first of all be a very stable ~100 m long optical bench
Drift stability of focused beam (ID01): 10-9-10-8 m / hour (Europe: few 10-6 m/h)

## Slide 35: Examples for coherent reconstruction
Thanks to V. Favre-Nicolin and S. Leake, wave font analysis is now “press the button”

## Slide 36: Examples for coherent reconstruction
Reconstruction of siemens star and later biological samples
Beamsize 150x350 nm
100 nm

## Slide 37: BRAGG CDI : REAL SPACE RECONSTRUCTIONS
Au particles:
M. Dupraz et al., Nano Letters Oct 2017

## Slide 38: CDI under Bragg conditions from catalytic nanoparticles
Iso-surface showing the strain
distribution inside the particle
Coherent reciprocal space image
S. Fernandez et al., submitted (2017).
SEM image of a single Pt nanoparticle
Spatial resolution: 10-20 nm, time resolution: many minutes..
More in the Talk of M.-I. Richard

## Slide 39: New sources for new challenges: the ESRF upgrade to an extremely brilliant source (EBS)
Increase of Brilliance: x40 (operational in 2020)

## Slide 40: Evolution of (DC-)Brilliance of Synchrotrons
Light sources: 12 orders of magnitude in 35 years
Brilliance of Future ESRF will do 12 orders of magnitude better than current laboratory sources.
0.1-10 KW per X-ray anode source
ESRF 2020 (10 % coherent)
Power consumption:
100 KW per beamline

## Slide 41: ESRF EBS: An ambitious new standard for synchrotron storage rings
Synchrotron X-rays
1024
1023
1022
1021
1020
1019
1018
1017
1016
1015
1014
1013
1012
1011
1010
109
108
107
106
1900 1920 1940 1960 1980 2000 2020
Brilliance (photons/s/mm2/mrad2/0.1%BW)
X-ray tubes
First generation
Second generation
Synchrotron Radiation
Third
generation
ESRF (2014)
ESRF (1994)
ESRF-EBS (2020)
ESRF Extremely Brilliant Source
ESRF-EBS – 150 M€ (2015-2022)
revolutionary design
for a new generation of synchrotron
source storage rings: ~100 times more brilliant and coherent X-rays
Programme to exploit the qualities of this new and unique extremely brilliant X-ray source:
- Creation of new beamlines
- Innovative detector programme
- « Data as a Service » strategy
The ESRF will operate until December 2018 and come back to user operation early/mid 2020
Ultimate synchrotron
Thank you for your attention!!

## Slide 42: OPERANDO STUDIES WITH FFXDM: SYNTHESIS OF M-O SOLAR CELL
Zhou, Reiss, et al
Annealing of a solvent deposited
metal organic perovskite solar cell during annealing at 115 °C
CTO
TiO2
MAPICl
SEM Cross section
Prominence of the (001) out of plane orientation during annealing

## Slide 43: Scanning probe spectroscopy in complex systems
Nanoparticles of Ag (medicine), ZnO and TiO2 (sun-screen) are very commonly used. Where do they end up ?
ID21 , M. Cotte, coll. University Ca’ Foscari, Venezia, M. Roman, W. Cairns and C. Rigo
Biopsies were obtained from the same patient during treatment (day 3, 6, 9 and 12)

## Slide 44
90% retained in the sludge most likely as Ag2S
Ag NPs Release from consumer products
In Europe 55% of this sewage sludge is applied on agricultural soils as a fertilizer
What are the properties of this nano Ag2S
in the environment?
Impact on soil quality/crops production ?
Transfer to the food chain ?
Larue et al. J Hazard Mater 264 (2014)
Uptake of Ag and Ag NPs in food crops
Pradas de Real et al., Env. Sci Technol., 2017
20 µm
parenchyma
epidermis
.
2
0 µm
.
.
100 µm
20 µm
stomata
Leaf surface
Leaf cross-section
Leaf cross-section
parenchyma
epidermis
stomata
stomata

## Slide 45: NEW TOOLS for new challenges
Blue dots: surface to cover twice the worlds primary energy demand by 15% efficiency photovoltaics
Wheat production per hectare land
Photovoltaic panel with 15 % efficiency: Annual yield of 300 kWh/m2
Brazil: 15 t of sugar per hectare (6 kWh/m2
Annual yield 4 t of ethanol~ 3 kWh/m2)
Needs:
-Improving power generation from non-fossil sources
-Power storage and management (conversion or batteries):
A vast field covering photocatalysis, electrocatalysis
and electrochemistry.
Notes: Burning what we eat can only be a temporary solution… Technologies have to overcome the other problems

## Slide 46: Beamlines of 2025+
Optics that adapt longitudinal coherence length to experiment.
Horizontal geometry for coherent Bragg diffraction may also work well at “higher energies”
Careful with high energies (even though tempting) “l4 -l7 law”:
Coh. flux ~B*l2; Beyond diff limit: “B~l”. Detector efficiency “~l”
Contraction of rec. space (malus or bonus) Iint~ l3
Enabling technologies:
Detectors and focusing optics (CMOS based detectors….)
Multilayer Laue lenses, diamond CRLs, …
Is that all ?

## Slide 47
MOTIVATION
CDI MAGING OF DEFECTS IN SINGLE NANOWIRES
2 µm
Etching revealed inversion domain boundaries (IDBs) separating domains with Ga- or N-polarity.
Pixel size : 16 nm X 8 nm
(Qx,Qy) cut: 004 GaN
Displacement between domains:
out-of-plane: (c/2+8 pm)
in-plane: 0 pm
S. Labat, M.I. Richard, M. Dupraz, et al., ACS Nano 9, 9210 (2015)
Notes: Displacements can be measured in picometers

## Slide 48: Strain imaging
GaN grown on pre-patterned sapphire
Sapphire
GaN
Bragg Intensity from GaN
Total strain variance:
1exp-3
Rotational variance (Tilt)
Data Courtesy: M. Nemoz, P. de Mierry, CRHEA/CNRS Antibes
Notes: Nucl.& trans. Layers, sounds easy but that’s where all the miracles have to happen.

## Slide 49: Scanning microdiffraction from Strained Ge Laser structure
Relaxation of the surrounding area as Ge is free to expand in the in-plane direction.
Compressive in plane and Tensile out-of-plane strain at the corners (0.032%).
SEM
10 µm
2 µm
Chahine et al. Appl. Phys. Lett 2015
Maximum Tensile out-of-plane strain on the bridge (0.1%).

## Slide 50: K-MAP& XSOCS: FROM EXPERIMENTS TO MEASUREMENTS
K-map:
The 1st ID01 workhorse
One command line starts a 1-3 hours K-Map (complete 5 D dataset)
D. Naudet, G. Chahine, S. Leake, M.I.-Richard, C. Richter
Examples:
Ristanovic Z., Angewandte Chem. 52, (2013)
Chahine G.A. et al. J. of Appl. Cryst. 47, (2014)
Richard M.-I. et al. ACS Appl. Mat. & Interf. 7, (2015)
Filippelli E J. Appl. Cryst. 49, (2016)
10 mm
T = 25°C
T = 400°C
Strain distribution in a Si device in the vicinity of a copper via
(Vianne et al. Appl. Phys. Lett 2015)

## Slide 51: THE K-MAP FAST SCANNING TOOL
Velocity: few hundred images/s
Limited by
-available flux
-mechanical limit of the stage/ trajectory
Real Space (2D)
Reciprocal space (3D)

## Slide 52: Tomorrows sources: what are the challenges ?
«airplanes are toys without any military value »
Marechal Foch (1851-1929)
The energy produced by the atom is a very poor kind of thing. Anyone who expects a source of power from the transformation of these atoms is talking moonshine.
Ernest Rutherford 1933
«in five years nobody will talk about the automobile anymore, I believe in the horse »
Wilhelm II. (1859-1941)
The inventers
The deciders
The users
If we have learned one thing from the history of invention and discovery, it is that, in the long run — and often in the short one — the most daring prophecies seem laughably conservative
A. C. Clarke

## Slide 53: BRAGG CDI : TOWARDS OPERANDO STUDIES
Before reaction
After (CO + H2)
reaction
Modification of Pt-Cu core shell Nanoparticles during reaction.
M.-I. Richard (ANR project CHARLINE)

## Slide 54: Local diffraction: advantages
Page 54
Bragg diffraction -> picometer precision
Small beams -> 100 nm spatial resolution
Combining small x-ray beams with diffraction: hybrid information on two lengths scales
Position 1: interatomic distance a
Position 2: interatomic distance b
X-ray diffraction micrograph
Intensity variations=
Thickness variations of 0.5 nm in the Si QW.
Measured without sample preparation.
P. Evans et al. Adv. Mater (2012)