## Slide 4
FOR ANY INFORMATION & HELP …
STEPHANIE
Pouget
JEROME
Faure-Vincent
DAVID
Djurado

## Slide 5
How large facilities can help to face
the numerous challenges lifted
by organic and hybrid electronics?
A general introduction.
David
DJURADO
INAC
CNRS – CEA Grenoble

## Slide 6
ORGANIC ELECTRONICS?
Powders or Free Standing films.
Doped conjugated polymers
Essentially research of stable metal-like materials by doping the conjugated polymers
Structure-conductivity relationship
Static and dynamic disorder effects
(Structural defects, crystallinity, preferred orientation but also vibrations, local dynamics and lattice dynamics contributing to charge carrier scattering)
X-rays and neutrons have been used
In 1989, we did the first measurements
of neutron scattering on oriented (CH)x (structure and dynamics).
D. Djurado, J. Ma, N. Theophilou, J.E. Fischer, Synth. Metals 30 (1989) 395
J.L. Sauvajol, D. Djurado, A.J. Dianoux, N. Theophilou, J.E. Fischer Phys.Rev. B 43 (1991) 14305.
Late 80’s, early 90’s

## Slide 7
Transport of electrical current, defects, static disorder, lattice vibrations
DELOCALIZED ELECTRON
LATTICE VIBRATION
APPLIED VOLTAGE
SCATTERED ELECTRON
ELECTRON LOCALIZED BY DEFECTS OR DISORDER
LATTICE VIBRATION
BAND TYPE CONDUCTION
CONDUCTION BY HOPPING
0 K
T
Notes: Quand les états électroniques sont localisés, la température et les vibrations du réseau qu’elle engendre n’agissent plus vraiment comme dans le cas d’un métal. Assistée par les vibration du réseau cette propoagation s’appelle conduction par sautsDans le cas le plus général, la conduction dans un fil moléculairen’est pas vraiment de la conduction par sauts, ce n’est pas non plus une conduction cohérente; c’est un processus intermédiaire dans lequel les vibrations du réseau favorisent et gênent à la fois la conduction.

## Slide 8
We think more and more directly in terms of electronic components, electronic devices, taking profit of n and p type semiconducting properties of conjugated polymers and small molecules.
Solar cells
OLED
NOWADAYS

## Slide 9
1
2
3
Bulk Heterojunction
Nanomorphology
Interfaces uneasy to be electronically and structurally characterized are involved and many other parameters have to be controlled.
The most complex arrangements are often the most effective in terms of devices performances

## Slide 10
Photo-induced charge transfer
P-type semiconductor
N-type semiconductor
Photon absorption
+
-
Creation
of exciton
Charges separation
Transport of e-
Transport of h+
Cathode
Anode
Bulk-heterojunction solar cells (BHJ)
Photo-induced charge transfer < 10-12 s
Heeger et al.Science, 1992, 258, 1474.
All the effects at interfaces are critical
Electrode/active material: injection of charges
N-type semiconductor/ P-type semiconductor: quality of charge separation
Minimizing charges recombination.

## Slide 11
p-type, n-type or ambipolar organic field effect transistors
Stacked layers with 50 < total thickness < 200 nm.
The substrate can be rigid or flexible.
That gave birth to flexible electronics which can be fabricated using printing processes (ink jet, roll to roll,…)

## Slide 12
Bottom-up processes of fabrication
Very important to master the solution phases, deposition and casting processes
For polymers the control of the molecular mass and the orientation of chains are often decisive for obtaining good performances of devices.

## Slide 13
Nowadays, large scale production of flexible printed circuits included in various devices is a reality.
OLEDs based TV sets and flexible displays for smartphones
Roll to roll process of fabrication of
flexible organic solar cells.

## Slide 14
This is definitively a multiscale story!!!
OPV
OFET
J. Rivnay et al., Chem. Rev. 112 (2012) 5488.

## Slide 15
It turns out that X-rays and Neutrons are radiations/particles which allow to explore the structure and the dynamics of matter in a very broad range of lengths and times.
Techniques of choice using these radiations are well adapted to the study of materials and devices of interest in the field of organic and hybrid electronics.
Let see in few minutes some basic aspects in order to feel better (?.. maybe….) when our speakers will show us more details……

## Slide 16
EPN Campus : ESRF, ILL, EMBL

## Slide 17
Synchrotron principle
1-2: Linear accelerator (LINAC)
3: Booster
4: Storage ring
5-6: Optics and experimental stations

## Slide 18
Insertion devices
Undulators
Focusing
Magnets
Bending
Magnets
Optics Hutch
Experimental Hutch
Control Hutch

## Slide 19
Insertion devices
Bending magnet
Undulator

## Slide 20
Some useful formulas for SR

## Slide 21
Production of neutrons
Nuclear reactor
(ILL Grenoble, Orphée Saclay, Berlin, Munchen)
Fission reaction Of 235U
Power of a scientific reactor is much smaller than that of nuclear electricity plant.
ILL 48 MW to be compared with 800 MW of each of 6 reactors in Fukushima.
n
n
n
n
Fission products
Energy release 1-2 MeV
Created neutrons are moderated in heavy water D2O
Energy is decreased from 1 MeV to few meV after several dm.
Depending on energies we speak about hot (≥ 100 meV), thermal (25 meV) or cold neutrons (≤ 10 meV)
Blue Cherenkov Emission.
Neutrons are produced as a continuous flux with a Maxwell distribution in energy.

## Slide 22
Production of neutrons
Spallation sources
ISIS GB, SINQ CH, ESS to come in Lünd Sweden
P
(1GeV)
p
p
n
(few MeV)
n
n
n
Also these produced neutrons need to be moderated
Muons and other particles are also produced.
Neutrons come on samples as a white pulsed beam
W nucleus

## Slide 23
Courtesy: F.W. Kuhs – Hercules course

## Slide 24
source
Detector
Scattering experiment: electronic density (with X-rays) or scattering length density (with neutrons) correlations probed along direction (only)
Courtesy: S. Pouget

## Slide 25
A large majority of fibrils are in the same orientation respectively to the substrate
q
2q

## Slide 26
Scattering experiment - basics
2q
l=1,54 Å
= 0,05 deg => d ~ 100 nm
q = 20 deg => d ~ 2 Å
d = 2p/ Probed distance in the sample
Synchrotron sources: l=0,1 – 100 Å (100 – 0.1 keV)
Neutron sources: l=0.04 - 30 Å (500 – 0.1 meV)
Source
Detector
Small Angle X-rays or neutron scattering
Wide Angle X-rays or neutron scattering
Courtesy: S. Pouget
Bragg relation gives

## Slide 27
Courtesy: M. Müller – Hercules 2014
d
(nm)
1
100
Q
(nm-1)
1
0,01

## Slide 28: Grazing incidence X-ray diffraction measurements (GIXRD)
Principle
In reflection (out-of-plane geometry)
This is a side view
The layer to be probed is typically from (30 to 400 nm thick)
a
2q

## Slide 29: Grazing incidence X-ray diffraction measurements (GIXRD)
In-plane geometry
This is a TOP view – q is contained in the plane
The detection plane is parallel to the plane of the sample
2q
a
a

## Slide 30: Grazing incidence X-ray diffraction measurements (GIXRD)
Crystallinity of the deposited layer
Preferred orientation of the deposited layer long axis ordering of polymers or molecules)
Mosaics : distribution in-plane or out-of-plane of chain or molecules orientation
Depth profiling of a given layer: evolution of the stacking mode of molecules from the first molecular layers on the substrate to the very surface
d
(Å)
1
30
Q
(Å-1)
1
0,03

## Slide 31
To travel through a multiscale world follow the guides !!!
J. Rivnay et al., Chem. Rev. 112 (2012) 5488.
Almost exclusively based on radiation scattering/diffraction
Measurements in the Q space.

## Slide 32
Synchrotron radiation properties
High energies (up to 500keV) ==> High penetration of X-rays in matter, non destructive bulk studies .
High flux, high brightness (109-1010 ratio compared to lab. X-rays sources) ==> Fast data acquisition < 5 ms (240 frames/s), can study fast and irreversible transformations (chemical kinetics, phase transitions…).
Very broad energy spectrum possible from IR to High energy X-rays, IR, UV, Raman spectroscopy possible.
Tunable incoming energy ==> Possibility for distinguishing chemical elements, x-rays absorption spectroscopy (XANES & EXAFS), anomalous scattering, tomography.
Very small spatial divergence of X-ray beam.
Can focus the X-rays beam to very small size (nowadays perspective is < 20 nm) ==> diffraction mapping, microscopy.
Polarized beam.
Temporal structure (in the storage ring different modes of filling are possible and packets of accelerated electrons are more or less numerous possibility to do kinematical studies)

## Slide 33
Historical evolution of X-rays sources brilliance

## Slide 34
Synchrotron radiation properties
High energies (up to 500keV) ==> High penetration of X-rays in matter, non destructive bulk studies .
High flux, high brightness (109-1010 compared to lab. X-rays sources) ==> Fast data acquisition < 5 ms (240 frames/s), can study fast and irreversible transformations (chemical kinetics, phase transitions…).
Very broad energy spectrum possible from IR to High energy X-rays, IR, UV, Raman spectroscopy possible.
Tunable incoming energy ==> Possibility for distinguishing chemical elements, x-rays absorption spectroscopy (XANES & EXAFS), anomalous scattering, tomography.
Very small spatial divergence of X-ray beam.
Can focus the X-rays beam to very small size (nowadays perspective is < 20 nm) ==> diffraction mapping, microscopy.
Polarized beam.
Temporal structure (in the storage ring different modes of filling are possible and packets of accelerated electrons are more or less numerous possibility to do kinematical studies)

## Slide 35
To travel through a multiscale world follow the guides !!!
J. Rivnay et al., Chem. Rev. 112 (2012) 5488.
To probe the material at distances longer
than 50 nm with different resolutions and
to image in the real space nano-or
micromorphology in 2D or 3D, other
experiments are possible :
Tomography
Phase contrast imaging
µ-fluorescence
Full field diffraction imaging
Coherent scattering (ptychography)
Resonant scattering of soft X-rays
Moreover, the possibility to tune the incident
energy allows to develop different
spectroscopies as:
X-rays absorption spectroscopy
X-rays emission spectroscopy
X-ray Raman scattering
Chiara Cavallari (ESRF)
chiara.cavallari@esrf.fr
X-rays spectroscopy

## Slide 36
To travel through a multiscale world follow the guides !!!
To probe the material at distances longer
than 50 nm with different resolutions and
to image in the real space nano-or
micromorphology in 2D or 3D, other
experiments are possible :
Tomography
Phase contrast imaging
µ-fluorescence
Full field diffraction imaging
Coherent scattering (ptychography)
Resonant scattering of soft X-rays
Moreover, the possibility to tune the incident
energy allows to develop different
spectroscopies as:
X-rays absorption spectroscopy
X-rays emission spectroscopy
X-ray Raman scattering
Julie Villanova (ESRF)
julie.villanova@esrf.fr
X-rays nanotomography

## Slide 37
To travel through a multiscale world follow the guides !!!
To probe the material at distances longer
than 50 nm with different resolutions and
to image in the real space nano-or
micromorphology in 2D or 3D, other
experiments are possible :
Tomography
Phase contrast imaging
µ-fluorescence
Full field diffraction imaging
Coherent scattering (ptychography)
Resonant scattering of soft X-rays
Moreover, the possibility to tune the incident
energy allows to develop different
spectroscopies as:
X-rays absorption spectroscopy
X-rays emission spectroscopy
X-ray Raman scattering
Peter Reiss (INAC)
peter.reiss@cea.fr
In situ measurement of crystal growth
of nanocrystals and perovskites layers at ESRF
Tobias Schülli (ESRF)
tobias.schulli@esrf.fr
Bragg diffraction based imaging techniques
Tao Zhou (ESRF)
tao.zhou@esrf.fr
The new full field diffraction x-ray microscope at ID01:
new possibilities for in situ and operando experiments

## Slide 38
To travel through a multiscale world follow the guides !!!
J. Rivnay et al., Chem. Rev. 112 (2012) 5488.
To probe the material at distances longer
than 50 nm with different resolutions and
to image in the real space nano-or
micromorphology in 2D or 3D, other
experiments are possible :
Tomography
Phase contrast imaging
µ-fluorescence
Full field diffraction imaging
Coherent scattering (ptychography)
Resonant scattering of soft X-rays
Moreover, the possibility to tune the incident
energy allows to develop different
spectroscopies as:
X-rays absorption spectroscopy
X-rays emission spectroscopy
X-ray Raman scattering
Marie-Ingrid Richard (ESRF)
marie-ingrid.richard@esrf.fr
X-rays coherent scattering and its future developments

## Slide 39
Synchrotron radiation properties
High energies (up to 500keV) ==> High penetration of X-rays in matter, non destructive bulk studies .
High flux, high brightness (109-1010 compared to lab. X-rays sources) ==> Fast data acquisition < 5 ms (240 frames/s), can study fast and irreversible transformations (chemical kinetics, phase transitions…).
Very broad energy spectrum possible from IR to High energy X-rays, IR, UV, Raman spectroscopy possible.
Tunable incoming energy ==> Possibility for distinguishing chemical elements, x-rays absorption spectroscopy (XANES & EXAFS), anomalous scattering, tomography.
Very small spatial divergence of X-ray beam.
Can focus the X-rays beam to very small size (nowadays perspective is < 20 nm) ==> diffraction mapping, microscopy.
Polarized beam.
Temporal structure (in the storage ring different modes of filling are possible and packets of accelerated electrons are more or less numerous possibility to do kinematical studies)

## Slide 40
To travel through a multiscale world follow the guides !!!
J. Rivnay et al., Chem. Rev. 112 (2012) 5488.
To probe the material at distances longer
than 50 nm with different resolutions and
to image in the real space nano-or
micromorphology in 2D or 3D, other
experiments are possible :
Tomography
Phase contrast imaging
µ-fluorescence
Full field diffraction imaging
Coherent scattering (ptycography)
Resonant scattering of soft X-rays
Moreover, the possibility to tune the incident
energy allows to develop different
spectroscopies as:
X-rays absorption spectroscopy
X-rays emission spectroscopy
X-ray Raman scattering
Nicolas Jaouen (SOLEIL)
nicolas.jaouen@synchrotron-soleil.fr
Soft X-rays (coherent) resonant scattering
and its potential in the field of
polymers and organic electronics

## Slide 41
Coherent diffraction imaging
P3HT/PCBM blend
hn=6.2 keV
(PCBM concentration)
PCBM concentration distribution
Phase contrast imaging
Patil N, et al. (2016) X-Ray Nanoscopy of a Bulk Heterojunction. PLoS ONE 11(7): e0158345. doi:10.1371/journal.pone.0158345
X-Ray Imaging -> back to real space
High resolution (>10nm)
Long counting time…
Courtesy: S. Pouget

## Slide 42
Resonent scattering of polarised soft X-Ray (P-SoXS)
=> Energy tuning at a value characteristic of Carbon p orbital
=> Playing with beam polarization
Donor/acceptor blend P3HT/P(NDI2OD-T2)
Collins B.A. et al, Nature Mater. 11, 536-543 (2012)
P-SoXS
hn=C1s->p*=285.3 eV
300
100
D=2p/q (nm)
Relative molecular orientations at the donor/acceptor interface deduced from P-SoXS data.

## Slide 43
Multi-scale character
Structure
Dynamics
NEUTRONS
Incoherent quasi-elastic and inelastic neutron scattering are very good probes to study the proton and lattice dynamics in the 10-13 – 10-9 s time range.
It can be said that this dynamic disorder is also quasi-intrinsic to organic media and it is, in my view, impossible to ignore the electron-phonon coupling effects to fully understand the properties of materials involved in organic and hybrid electronics

## Slide 44
A quasi-elastic neutron scattering experiment
Time of flight spectrometer
Sample
Detector
Detector
k
0
Inelastic Scattering
E
2
>
E
0
k
2
>
k
0
k
2
Q
2
k
1
Inelastic Scattering
E
1
<
E
0
k
1
<
k
0
Q
1
Elastic Scattering
E
=
E
0
k
=
k
0
Q
k
Incoming Neutrons
Energy
E
0

## Slide 45
The number of scattered neutrons as a function
of the energy exchange is measured.
One spectrum in energy is obtained for each value of Q (or q).

## Slide 46
Mohamed Zbiri (ILL)
zbiri@ill.fr
Introduction to Quasielastic and Inelastic Neutron
Scattering, and Role of Atomistic Simulations

## Slide 47
Anne A.Y. Guibert et al.,
Chem. Mater. 2015, 27, 7652 - 7661
Osiris
IN16
Anne Guilbert (Imperial College)
a.guilbert09@imperial.ac.uk
Insight in the dynamics of organic photovoltaic active
layer: a combined approach of neutron scattering and
atomistic simulations

## Slide 48
I declare
open !!!!