## Slide 1: Structure and dopant engineering in PEDOT thin films for thermoelectric applications
Magatte Niang GUEYE
PhD student
magatte.gueye@cea.fr
December 4., 2017
Liten:
Dr. Alexandre CARELLA
Dr. Etienne YVENOU
Amélie Schultheiss
Dr. Nicolas MASSONNET
Sophie BRENET
Dr. Anass BENAYAD
Dr. Jean-Pierre SIMONATO
INAC:
Dr. Jérôme FAURE-VINCENT
Dr. Stéphanie POUGET
Dr. François RIEUTORD
Dr. Hanako OKUNO
Dr. Renaud DEMADRILLE

## Slide 2: Plenty of energy is wasted…
Around 90% of primary energy is first converted to heat
J Cullen et al., Energy, 2010, 35, 2059

## Slide 3: Mostly at t below 100 °c
60 % of heat losses are at temperature below 100°C
C. Forman et al., Renew. Sust. Energ. Rev., 2016, 57, 1568-1579

## Slide 4: motivation
Why is it important to harvest such energy (lost anyway) ?
Possible with thermoelectric devices

## Slide 5: Thermoelectric devices
+
+
+
+
+
+
+
+
+
+
+
Figure of merit
  Requirements for a good efficiency
      A high Seebeck coefficient S
      A high electrical conductivity σ
      A low thermal conductivity λ
      S = Seebeck coefficient (ΔV/ΔT)
      σ = electrical conductivity
      λ = thermal conductivity
ΔV = S ΔT > 0 for a p-type and < 0 for an n-type semiconductor

## Slide 6: Thermoelectric materials
  Intrinsic thermoelectric properties  specific temperature range of utilization
  RT performant thermoelectric materials: Te based
      Scarce
      Toxic
      Expensive (material & process)
  Need of new alternatives
   Organic materials
n-type
p-type

## Slide 7: Organic semiconductors
Main applications
Organic Light Emitted Diode (OLED)
Organic Photovoltaics
(OPV)
Organic Thin Film Transistor (OTFT)

## Slide 8: Organic and Hybrid Materials as ThErmoelectric Materials
Moderate electrical conductivity
Low thermal conductivity (0.2 – 0.5 W.m-1.K-1)
Limited temperature range
(<200 °C)
Widely tunable thermopower
Possibility of adding thermoelectric inclusions
4 décembre 2017
| PAGE 8
CEA | December 4., 2017
S
S²σ
σ
1014 1015 1016 1017 1018 1019 1020 1021 1022
Charge carrier concentration (cm-3)
S, σ, S²σ
Insulators
Semiconductors
Metals

## Slide 9: Strategy to improve zt
2
Intrinsically low λ
Given temperature range
Improving the power factor PF = σS²
σ and S linked through the charge carrier concentration
1
Improving the electrical conductivity
Improving the Seebeck coefficient
Better ordered structure (mobility)
Reduction (charge carriers)
N. Massonnet, A. Carella et al., J. Mater. Chem. C, 2014, 2, 1278
S. Patel, M. Chabinyc, J. Appl Polym. Sci., 2017, 134, 44403

## Slide 10: Starting material: PEDOT:PSS as TE material
Poly(3,4-ethylenedioxythiophene)
+
poly(styrene sulfonate)
Dispersion in water (hydrophilic PSS)
Primary doping induced by PSS
Secondary doping by dipping in ethylene glycol (EG) and annealing
σ = 1000 S/cm
Seebeck coefficient : 18 µV K-1

## Slide 11: Improving the electrical properties
  PEDOT:OTf
      σ = 1218 S.cm-1
  N. Massonnet, A. Carella et al., Chemical Science, 2015, 6, 412
1
Smaller counter ions
F
F
F
SO3
F
F
F
SO3
Solvent treatment
Acid treatment
2
3
Jingkun Xu et al., Adv. Electron. Mater., 2015, 1, 1500017

## Slide 12: Experiments & characterization
Cosolvent addition
Oxidative solution
PEDOT:OTf-NMP film
NMP addition
Acid treatment
Substrate (glass)
PEDOT:OTf-NMP film
Substrate (glass)
PEDOT:Sulf-NMP film
Film deposition
Oxidative solution
Addition of EDOT
Spin coating
Substrate (glass)
Non fully oxidized deposited film
Substrate (glass)
PEDOT:OTf film
EDOT formulation
Heating @ 70°C

## Slide 13: Effect of co-solvent addition
 Optimum co-solvent concentration
UV-Vis-NIR spectroscopy
Without NMP
With NMP
UV-Vis-NIR of oxidative solution with and without NMP
 Polymerization rate slowed down

## Slide 14: Origin of the increase in σ
Cosolvent addition
Oxidative solution
PEDOT:OTf-NMP film
NMP addition
Polymerization rate slowed down
What about the acid treatment ?
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 15: Effect of acid treatment
Materials | PEDOT:OTf-NMP | PEDOT:Sulf-NMP
Sulf/Thiophene ratio | 39 % | 64 %
Conductivity | 3630 S.cm-1 | 5462 S.cm-1
PEDOT:OTf-NMP
PEDOT:Sulf-NMP
XPS on

## Slide 16: Origin of the increase in σ
Cosolvent addition
Oxidative solution
PEDOT:OTf-NMP film
NMP addition
Acid treatment
Substrate (glass)
PEDOT:OTf-NMP film
Substrate (glass)
PEDOT:Sulf-NMP film
• Polymerization rate slowed down
• Replacement of triflate ions by sulfate ones
• Redox state ↑
What impact on the structure of the film ?
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 17: Structure – X rays (ESRF BM 32 – Rigaku)
Lamellar stacking
(π) stacking
(100)
q = 0,46 Å-1
d = 13,5 Å
(020)
q = 1,85 Å-1
d = 3,4 Å
Edge-on
PEDOT:OTf
PEDOT:OTf-NMP
PEDOT:Sulf-NMP
Our lab, somewhere here
Beautiful mountains all around
Bigger cristallites are grown (longer chains ?)
The structure is tighter packed
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 18: Structure - HRTEM
π-stacking : 3,6 Å
Chain length information
X-rays values verified
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 19: Origin of the increase in σ
Cosolvent addition
Oxidative solution
PEDOT:OTf-NMP film
NMP addition
Acid treatment
Substrate (glass)
PEDOT:OTf-NMP film
Substrate (glass)
PEDOT:Sulf-NMP film
• Polymerization rate slowed down
• Replacement of triflate ions by sulfate ones
• Redox state
• Bigger crystallites
• Longer polymer chains
• Better stacking
• Better stacking
How do the chains’ organization and the dopant influence the transport mechanisms ?
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 20: Transport properties – σ = f(t)
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462, 3462
PEDOT:OTf
PEDOT:Sulf
PEDOT:OTf-NMP
PEDOT:Sulf-NMP
Structure + Metallic behavior @ 0 K and RT + charge carrier nature  common VRH  Metallic conduction
Structure + metallic conduction + Disordered region  disordered metallic conduction
Structure + W  0  Sheng’s conduction model
Heterogeneous conduction model

## Slide 21: Transport properties – σ = f(t)
Metallic
Sheng
Disordered
Metallic
PEDOT:OTf
PEDOT:Sulf
PEDOT:OTf-NMP
PEDOT:Sulf-NMP
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 22: Transport properties – σ = f(t)
PEDOT:OTf
PEDOT:Sulf
PEDOT:OTf-NMP
PEDOT:Sulf-NMP
Quasi 1D metal + Fluctuation Induced Tunneling // Disordered metal
σ=2660 S cm-1 (+166%)
σ cristallites +140%
σ amorphe +167%
σ=4500 S cm-1 (+69%)
σ cristallites -8%
σ amorphe +73%
σ=1000 S cm-1
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 23: Origin of the increase in σ
Cosolvent addition
Oxidative solution
PEDOT:OTf-NMP film
NMP addition
Acid treatment
Substrate (glass)
PEDOT:OTf-NMP film
Substrate (glass)
PEDOT:Sulf-NMP film
• Polymerization rate slowed down
• Replacement of triflate ions by sulfate ones
• Redox state
• Bigger crystallites
• Longer polymer chains
• Better stacking
• Better stacking
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462
• Quasi 1D metallic conduction which increases in the cristallites as well as in the disordered domains
• The sulfuric acid impacts the disordered domains (increase of oxidation level and replacement of triflate counterions)

## Slide 24: Conclusion
PEDOT:OTf
σ = 1218 S.cm-1
PEDOT:OTf-NMP
σ = 3630 S.cm-1
      Increase of structural order
      Increase of grain size
      Increase of oxidation level (acid treatment)
      Increase conduction in amorphous PEDOT
      Metallic behaviour + optimized disorder
PEDOT:Sulf-NMP
σ = 5462 S.cm-1
Small counter-ions
Slower polymerization rate
Triflate substitution
Oxidation level ↑
PEDOT:PSS
σ = 0.1 S.cm-1
Big counter-ions
Excess counter-ions
Non treated
M. Gueye, A. Carella et al., Chemistry of Materials, 2016, 28, 3462

## Slide 25: Direction Département Service
Commissariat à l’énergie atomique et aux énergies alternatives
Centre de Grenoble
DRT/Liten/DTNM/SEN/LSIN
Contacts:
Alexandre.carella@cea.fr
Magatte.gueye@cea.fr
Thank you !
Questions / comments ?
Liten:
Dr. Alexandre CARELLA
Dr. Etienne YVENOU
Amélie Schultheiss
Dr. Nicolas MASSONNET
Sophie BRENET
Dr. Anass BENAYAD
Dr. Jean-Pierre SIMONATO
INAC:
Dr. Jérôme FAURE-VINCENT
Dr. Stéphanie POUGET
Dr. François RIEUTORD
Dr. Hanako OKUNO
Dr. Renaud DEMADRILLE

## Slide 26: Perspectives
* J. Coleman et al., ACS Nano, 2010, 4
PEDOT:OTf
σ = 1218 S.cm-1
PEDOT:OTf-NMP
σ = 3630 S.cm-1
PEDOT:Sulf-NMP
σ = 5462 S.cm-1
PEDOT:PSS
σ = 0.1 S.cm-1
187 Ω/□ @ 96.9 %, FOM* = 63.5
85 Ω/□ @ 91.7 %, FOM = 50
50 Ω/□ @ 84.9 %, FOM = 44
Transparent electrodes
Power Factor
177 µW.m-1.K-2
Organic thermoelectricity
BH solar cells
PCE : 0.59%, VOC : 0.54 V, JSC : 4.03 mA.cm-2 , FF 0.27
Organic photovoltaics

## Slide 27: Need of highly conductive PEDOT
  Commonly used in organic electronics
  Dispersible in water & commercial
X. Crispin et al, Nature Materials, 2011, 10
L. De Arco et al., ACS Nano, 2010, 4
H. Kang et al., Nature Communications, 2015, 6
Ö. Usluer, Journal of Materials
Chemistry C, 2014, 2
Notes: Özlem Usluer, J. Mater. Chem. C, 2014, 2

## Slide 28: Effect of acid treatment
  Increase of bipolaronic charge carriers
       increase of a semi-metallic behavior
  Crispin et al., Nat. Mater. 2013, 13, 190-194
Neutral chains
Polarons
Bipolarons
 | D(020) - Å | D(100) - Å
PEDOT:OTf | 40 | 75
PEDOT:OTf-NMP | 50 | 90
PEDOT:Sulf-NMP | 55 | 100
Film thickness !!

## Slide 29: thermoelectricity
  Three thermoelectric effects
      Seebeck (converting a temperature gradient into a voltage gradient), 1821 Thomas Johann Seebeck
      Peltier (converting a voltage gradient into a temperature gradient), 1834, Jean Charles Athanase Peltier
      Thomson (conductor heating / cooling), 1851, Lord Kelvin
Energy harvesting
  Clemens Forman et al., Renew. Sust. Energ. Rev., 2016, 57, 1568-1579

## Slide 32: Conjugated polymers
  Intrinsically low λ (0.1 ~ 0.5 )
  Tunable S:
      Doping: insertion of charges
  Tunable σ:
      Doping: insertion of charges
      Improvement of carrier mobility
Figure of merit & Power factor
P-type
Toshima, Synthetic Metals, 2007, 157, 467-474
Poudel, Science, 2008, 320, 634-638
Segalman, Nanoletters, 2010, 10,4664-4667
Crispin, Nature Materials, 2011, 10, 429-433
Sun, Advanced Materials, 2012, 24, 932-937
Kim, Energy and Environmental Science, 2013, 6, 788-792
Pipe, Nature Materials, 2013, 12, 719-723
Grunlan, Advanced Materials, 2015
Grunlan, Advanced Energy Materials, 2016
N-type
Sun, Advanced Materials, 2012, 24, 932-937
Yu, Advanced Materials, 2015
Koumoto, Nature Materials, 2015, 14

## Slide 33: Effect of co-solvent addition
 Optimum co-solvent concentration
Without NMP
With NMP
 Polymerization rate slowed down

## Slide 34: Improving the electrical properties
  PEDOT:OTf
      σ = 1218 S.cm-1
  N. Massonnet, A. Carella et al., Chemical Science, 2015, 6
F
F
F
SO3
F
F
F
SO3
J. Xu et. Al, Advanced Electronic Materials, 2015, 1
Strategy
  Improving the electrical conductivity through :
    Solvent treatment
    Acid treatment
  Material characterization

## Slide 35: Experiments & characterization
Cosolvent addition
Oxidative solution
PEDOT:OTf film
NMP addition
Acid treatment
Substrate (glass)
PEDOT:OTf-NMP film
in CH3NO2
Substrate (glass)
PEDOT:OTf-Ox film
Proportions
Oxidative solution without NMP: PEG-PPG-PEG + EtOH (20 + 80 wt. %) + FeOTf3 (126mg/ml)
Oxidative solution with NMP: add x wt. % NMP (x = 7.75, 8 or 8.5 depending on the humidity level)
PtCl4 : 2.5 M in nitromethane, filtered
Film deposition
Oxidative solution
Addition of EDOT
Spin coating
Substrate (glass)
Non fully oxidized deposited film
Substrate (glass)
PEDOT:OTf film
EDOT formulation
Heating @ 70°C
Heating @ 70°C